## Slide 1: Nanocrystals inside Ferritin inside Photovoltaic Cells
Kameron Hansen, Brigham Young University
Co authors:
John Colton (advisor)
Richard Watt (advisor)
J Ryan Peterson
Cameron Olsen
Alessandro Perego
Luis Perez
Heather Hogg

## Slide 2: Before I joined the group… there was a hypothesis
Ferritin
Reference: J. Mater. Chem. A, 2014, 2, 20782-20788
12 nm
12 nm
8 nm
8 nm

## Slide 3: Dye Sensitized Solar Cell
Semiconductive dye on porous TiO2
Electrolyte
Reference: Nature Chemistry 3, 188–189 (2011)

## Slide 4: Power efficiency of PbS nanocrystals
Voltage (mV)
Current (mA)
 | η (%)
Control | 0.43
Staining method 1 | 0.26
Staining method 2 | 0.28
Staining method 3 | 0.11

## Slide 5: Attention Diverted...
Advanced Materials 20.19 (2008)
Hennequin, et al.

## Slide 6: 2 main results:
1 – Simplified synthesis of PbS nanocrystals inside ferritin
2 – Achieved synthesis of PbSe nanocrystals inside ferritin

## Slide 7: PbS and PbSe inside Ferritin
Inhibit growth of cancerous cells
Catalyst in hydrogen evolution
Biological Imaging

## Slide 8: Colloidal Synthesis
After Sulfur/Selenium
Ferritin in Sodium Acetate
Lead
Sulfur/Selenium
After Lead

## Slide 9: Simplified PbS
Measured Lead per Ferritin
Targeted Lead per Ferritin
Anaerobic
Aerobic
Room Temp. Photoluminescence
2.25 nm
3.03 nm
6.10 nm
Photon Energy (eV)

## Slide 10
PbSe Size-Filtration Gel
Lead
Protein
Concentration
Fractions 1-10 (by size)

## Slide 11: PbS inside Ferritin PbSe inside Ferritin
20 nm
5 nm
20 nm
Ferritin Protein
Ferritin Protein
PbS Core
PbSe Core

## Slide 12: Conclusion - 2 main results
1 - Simplified PbS synthesis
2 - Achieved PbSe synthesis
Future work:
Optimize PbSe synthesis
Dye sensitized solar cell fabrication
Notes: 1) Developing synthesis of PbSe
2) Simplified the synthesis of PbS