## Slide 1: Optically detected magnetic resonance of silicon vacancies in SiC
Kyle Miller, John Colton,
Samuel Carter (Naval Research Lab)
Brigham Young University Physics Department

## Slide 2: Background: Defects in SiC
The goal is to use silicon carbide defects for quantum information purposes (qubits)
  SiC is cheaper than diamond and can be grown on a lattice
Defects occur where a silicon atom is missing
Determine spin coherence time of electrons in defects
From Riedel et al., Phys. Rev. Lett. 109, 226402 (2012)

## Slide 3: Background: Electron spins and ODMR
Laser promotes electrons to higher energies
Non-radiative transition causes the ms=1/2 state to populate faster
Microwaves equalize spin populations, causing a decrease in the observed photoluminescence (PL)
4A
4E
1/2
3/2
1/2
3/2
Metastable
doublet
See P. G. Baranov et al., Phys. Rev. B 83, 125203 (2011)
optical
Non-radiative
2D
B
ms=+3/2
ms=-3/2
ms=+1/2
ms=-1/2
S=3/2 system
Energy
From Sam Carter

## Slide 4: Experimental Setup
Place sample in cryostat, temperature as low as 6 K
Electromagnet provides localized field of up to 1.36 T
Microwave source combined with amplifier outputs more than 25 W
0.7 W of 870 nm laser hitting the sample
µwave
source
Cryostat
Electro-
magnet
B0
Bµwave
SiC
Laser

## Slide 5: Maximizing microwave power
Coupling loop is made from the inner conductor of the coax
Sample placed directly on the copper cold finger
B0
Bµwave
SiC
Laser

## Slide 6: Maximizing microwave power
Stub tuners, or “slide trombones”, help tune standing wave patterns
They match the impedance of the loop for maximum radiation output
Double stub
Single stub

## Slide 7: ODMR
Two resonant peaks, one varies in strength
Linear field dependence
Very close to 2

## Slide 8: ODMR – Microwave power
Increased response with increased microwave power
Width also increases

## Slide 9: Rabi oscillations
These occur when electrons are switched continuously up and down between spin states (See video)
Stronger microwave power means faster oscillations
This gives and pulses (which flip spins upside down and half-way upside down)
Laser
Laser
Vary length
(0 – 1000 ns)
1 µs
5 µs
207 MHz
250 MHz

## Slide 10: Spin echo
Laser
Laser
2 µs
20 µs
Set , then vary to observe the signal
Microwave pulses manipulate spin orientation
Signal is seen when pulses are equally spaced
"HahnEcho GWM" by GavinMorley - Gavin W Morley. Licensed under Creative Commons Attribution-Share Alike 3.0 via Wikimedia Commons - http://commons.wikimedia.org/wiki/File:HahnEcho_GWM.gif#mediaviewer/File:HahnEcho_GWM.gif
See video

## Slide 11: Spin echo data
Exponential decay of the signal predicts
Important figure is the percentage of the way toward 0

## Slide 12: Calculating T2
Fitting the exponential decay of the spin echo signal gives T2
Echo signal, 40 K

## Slide 13: Summary
Spin coherence time
Is this long?
  Pretty good. Long for GaAs, not super long for diamond
Can we get longer?
  Apparently not with temp, maybe with defect concentration
  What is the limiting factor on the lifetime?
Future work
Try different samples with varying amounts of defects from irradiation
NSF Grant PHY1157078